## Slide 1: Making a Wood and Resin Table
Keys to Success

## Slide 8: Downside of Resin
Messy
  sticky when liquid
  static charge to dust and shavings

## Slide 9: Downside of Resin – Con’t
Expensive - $17/ quart = $42.50/ bdf
Can be Stressful
  Mold leaks
  Curing problems - overheating

## Slide 10: Why use Resin?
Allows the use of beautiful wood that might not otherwise be usable
  Fill cracks and voids
  Show off natural edges

## Slide 11: Resin
Superclear 2.0 Liquid Glass Deep Pour Epoxy

## Slide 12: Safety
Generally considered non-hazardous
  Possible skin and eye irritant
Use in a ventilated area
Avoid skin contact
  Gloves and protective clothing
Dust mask when planing and sanding

## Slide 13: Wood Selection and Layout
Choose wood you love
1 ½” minimum thickness
Create a frame – rigid or loose strips

## Slide 15: Wood Selection and Layout – Con’t.
1” oversize
Key – All edges next to epoxy must be natural
No Straight cuts
Cutting a curve likely won’t substitute for natural edge

## Slide 16: Slab Preparation and Clean-up
Edges must be clean – No dirt, NO BARK
Tools
  Screwdriver
  Wire wheel – aggressive
  Nylon wheel
  Restorer
  Dental picks
  Dremel
Vacuum thoroughly

## Slide 19: Building a Mold
Base – ¾” Melamine
Sides ( 3-4” high) on top of the base
Pocket hole screws to hold the sides in place
Caulk between the edge of the side piece and base
  DAP Alex Fast Dry caulk

## Slide 22: Building a Mold – Con’t.
Key – CAULK ALL CORNERS – allow 24 hr cure
Key – USE MOLD RELEASE – don’t spray indoors
Smooth-On Universal Mold release

## Slide 23: Seal your slab
Sealing prevents staining – especially when using liquid dye
Sealing prevents bubbles – air released from wood
Use Deep Pour Epoxy - Paint top, bottom, sides and ends
Sealing the Top helps prevent warping during curing – stops moisture transfer
Put slab in mold to begin curing
Let set until tacky: 12 – 18 hours – still creates chemical bond

## Slide 25: Seal your slab - Con’t.
Spalted or other soft wood
  Table Top epoxy – 2 to 3 coats may be needed to seal
  Cure until hard – 24 hours
  Sand thoroughly – creates mechanical bond
  Clean surface with isopropyl alcohol

## Slide 26: Set up your mold
Elevate your mold - need airspace beneath it
Clamp your wood in place – wood floats in resin
Level your mold – door shims work well

## Slide 27: Mixing resin
Measure carefully – 2:1
Flat bottom bucket – 5 gallon
Key - Poor mixing = Failure - no way to recover
  Cannot overmix Deep Pour epoxy
Mixing time – minimum 5 mins. I mix for 10 minutes
Low speed paddle mixer – drill works great
Scrape the sides and bottom - rotate the bucket

## Slide 28: Add color to resin
Liquid dyes and powdered pigments
Liquid – solid color
Pigment – swirls
Check density of color – clear cup
Account for fastening hardware
Mixed resin should sit for 20 minutes – allows air bubbles to release
  Use a torch or heat gun to remove surface bubbles

## Slide 29: Pouring resin and monitoring your pour
Pour in the morning - all day to monitor
Ambient temp – 60 - 75 degrees
Brush the edges – releases air bubbles
Leak Repair – Rec. Flex Paste
Key – Always set a fan to ripple the liquid epoxy surface
  Removes heat from the pour to prevent overheating
Check pour depth - Add resin as needed
Check for bubbles – torch as needed
Pigment settles -Stir at 12 – 24 hours

## Slide 31: Remove the table from the mold
Cure time – initially 5 days
Full cure – minimum 2 weeks; 3 weeks better
Mallet to knock off the sides from the form
  Wear gloves – resin edges are sharp
Stiff blade putty knife to separate a corner from the mold
  Stiff plastic shims follow the knife

## Slide 32: Flatten and square the table top
Commercial
  Planer/Drum sander combo
  CNC
Drum sander for small table – can be slow
Router sled
  Can be shop built
  Can accommodate almost any size top
  Very messy; slow
Trim sides and ends
  Track saw
  Plywood strip clamped in place and circular saw

## Slide 34: Touch-ups
Top will have small chips in resin & possible voids in wood
Table Top epoxy to fill larger chips and voids
  Clear works well even with dyed or pigmented resin
  Cures in 24 hours
Very small remaining chips
  Fill with CA glue followed by activator; cures hard instantly

## Slide 35: Sanding
Key – Evenly sand the entire surface. Don’t focus on problem areas
  Draw a pencil grid across the entire surface to track sanding
Goal: Even scratch pattern after each grit
Preferred Sand paper - Cubitron 3M Extract
  Very durable and resists clogging
Use a progression of grits
  120, 150, 180, 220
  Go to 320 and 400 on resin
Use micro fiber cloth to wipe every few seconds as you sand
  Helps prevent clogging

## Slide 36: Questions